|  |  |  |
| --- | --- | --- |
| Magnesium oxide wafer | Factory sample | After treatment |
| Arithmetical mean height | 367 nm | 4 nm |
| Maxiumum height | 3.967 µm | 0.546 µm |
| Developed interfacial area ratio | 53.4 % | 0.0069 % |